## Slide 1
Shipment of Lithium Batteries
Technology Concept, Development and Testing
Jonathan Green
The statements contained herein are presented in good faith
for general information only.
AkroFire

## Slide 2
AkroFire
AkroFire is a solutions-oriented engineering company specializing in fire and thermal management for the Aerospace Industry.
Products and services cover OEM, Aftermarket and Defense.
This expertise has led to the development of a wide range of products and services including repair products for aircraft maintenance, interior products, high temperature insulation systems, firewall and fire hard composites and hazardous material packaging solutions
Shipment of Lithium Batteries

## Slide 3
Background
PHSMA Rule HM224B defined performance parameters for the packaging of Oxygen Cylinders and Oxygen Generators:
Prevent Flame Penetration
(1700oF / 5min – pt.III.AppF.par(a)(3)/(f)(5) 14CFRpt25)
Prevent Ox cylinder/generator from reaching critical temperature in an environment of 400oF for 3 hours
(Critical temperature being the auto vent or ignition temperature)
In response to this Akro developed a range of ‘Fire/Thermal Pack’ technologies and together with Americase developed a complete range of HM224B packaging solutions.
Shipment of Lithium Batteries

## Slide 4
Shipment of Lithium Batteries
Future HazMat packing challenge: Lithium Batteries
FAA Analysis summarized in:
Fire Protection for Shipment of Lithium Batteries / Equipment containing Lithium Batteries.
Report cited the performance of an Oxygen Generator Overpack as and effective containment for 18650 Lithium-ion cells.

## Slide 5
Overpack performance parameters:
1. Protect batteries from external fire: direct flame impingement
2. Protect batteries from heat: halon suppressed cargo fire
3. Containment: Prevent a battery thermal runaway from affecting adjacent shipments
Shipment of Lithium Batteries

## Slide 6
Concept
Develop an ‘overpack’ method that utilizes a free-flowing, loose fill “Packing Nut”
that following exposure to significant heat / fire
forms a contiguous rigid protective barrier.
Key properties:
Heat absorption
Heat resistance
High temperature stability
Gap filling
Versatility
- allow the use of ‘common’
packaging that is in regular
industry use.
ie standard HazMat boxes
Shipment of Lithium Batteries

## Slide 7
Shipment of Lithium Batteries
Early testing was performed on Lithium –ion rechargeable batteries, specifically :
AA (1.5v) and 18650 (3v) cells.
Performance was promising , showing good protection and containment.
-Results were presented at the May 2013 FAA Systems Meeting in Cologne.
Current developments center on using CR123 3v 1550mA.hr cells as the test article
CR123 cells selected because:
Highly energetic
Readily available
provide plenty of containment ‘challenges’ (!)
Render more conservative testing when
compared to Li-ion

## Slide 8
Typical Shipment Configuration
Develop the loose fill concept
Screen performance by utilizing CR123 cells
Define performance against test parameters identified in the FAA report.
Refine the product to optimize
Performance
Weight
Cost
Shipment of Lithium Batteries

## Slide 9
Typical Shipment Configuration
Shipment of Lithium Batteries
Battery OEM packing - loose fill –
HazMat box

## Slide 10
Range of tests:
Direct Flame Impingement: prevent the packed batteries from the effect of exposure to flame.
Thermal Protection: protect the packed batteries from the thermal effects of a controlled cargo compartment fire.
Contain thermal runaway: prevent the thermal and fire threat to adjacent packages
- Smoke leaking through seals is acceptable
    Fire or flames escaping is not acceptable
    Packing must maintain its structural integrity
Shipment of Lithium Batteries

## Slide 11
Direct flame impingement
Shipment of Lithium Batteries
Cargo liner test (1700oF / 5min – pt.III.AppF.par(a)(3)/(f)(5) 14CFRpt25) is primarily a materials test
For the purposes of this research, fully packaged test articles are used, with a representative fire load

## Slide 12
Direct flame impingement
Fire Load:
‘Park’ oil burner in horizontal configuration.
Burner throttled to:
Heat Flux: 7.5BTU(ft2sec) / 8.6W/cm2
Flame Temp: 1600oF / 871oC
(generally as per requirements of FAR25.855)
Shipment of Lithium Batteries

## Slide 13
Shipment of Lithium Batteries
Direct flame impingement
Test article: 100 x Lithium –metal CR135 cells
Inner box: single wall 7” x 7” x battery depth
Outer box: UN rated HazMat double wall cardboard 14.2” x 14.2 ”x 7.6”

## Slide 14
Shipment of Lithium Batteries
Direct flame impingement

## Slide 15
Maximum ‘battery’ temperature after 5 min = 92oF / 33oC
Shipment of Lithium Batteries
Direct flame impingement

## Slide 16
Shipment of Lithium Batteries
Direct Flame Impingement - Post- Burn

## Slide 17
Suppressed cargo fire – Thermal Resistance Test
General parameters as per PHSMA Rule HM224B:
400oF / 204oC Environment for 3 hours. Temperature is the estimated mean temperature of a cargo compartment during a halon suppressed fire. The time period is representative of the maximum estimated aircraft diversion time.
Critical internal temperature is the point at which thermal runaway is initiated:
Lithium Metal: ~350oF
Lithium-ion: ~ 450oF
Lithium –polymer: ~ 330oF
Shipment of Lithium Batteries

## Slide 18
Suppressed cargo fire – Thermal Resistance Test
Environment provided by air circulating oven.
Independent thermocouples monitor:
Battery Temperature
Oven Temperature
Box details:
Inner box: single wall 7” x 7” x battery depth
Outer box: UN rated HazMat double wall cardboard 14.2” x 14.2 ”x 7.6”
Shipment of Lithium Batteries

## Slide 19
Suppressed cargo fire – Thermal Resistance Test
Shipment of Lithium Batteries
Inner packaging
HazMat Box filled
Test article complete

## Slide 20
Suppressed cargo fire – Thermal Resistance Test
Maximum temperature of Cells = 202oF / 94oC
Shipment of Lithium Batteries

## Slide 21
Suppressed cargo fire – Thermal Resistance Test
Shipment of Lithium Batteries
Post test
Box opened –
note fused packing nuts
Inner box removed

## Slide 22
Thermal runaway
Shipment of Lithium Batteries
Battery runaway is a challenge:
Lithium metal appear to be the most severe and therefore represent an ideal threat
for the purposes of R&D
Thermal runaway characteristics:
Venting, with smoke, followed by flame, if ignited.
Rapid and large temperature rise, to 1500oF and higher
Sparks and flame jets
Smoke emitted is flammable

## Slide 23
Thermal Runaway
Shipment of Lithium Batteries

## Slide 24
Thermal runaway – CR123A Batteries
Shipment of Lithium Batteries
Stage 1:
Volatile components vent from cell. Resulting smoke or mist will ignite if there is air (oxygen) and a source of ignition.
Stage 2:
Internal cell components mix to produce a violent exotherm
High heat release in the cell, resulting in cell temperatures up to 2000ºF and beyond; also sparks and flame jets
Stage 3:
Propagation to adjacent cells, resulting in increasing conflagration

## Slide 25
Thermal runaway
Shipment of Lithium Batteries
Containing a thermal runaway:
Investigate loose fill volume requirements for a given battery quantity:
Thermal runaway initiated with a 75watt cartridge heater inserted into the test group.
Cartridge heater is disconnected once runaway is initiated.
Increasing quantity of cells tested
16 Cells
30 Cells
100 Cells
300 Cells
Broad spectrum of results used to define fill characteristics:

## Slide 26
Thermal runaway
Shipment of Lithium Batteries
Test article: 300 x Lithium –metal CR135 cells
Inner box: single wall 7” x 7” x battery depth – 3 stacks
Outer box: UN rated HazMat double wall cardboard 15” x 15 ”x 15”
Effective density of loose fill packing = 3.9lb/ft3
Inner boxes separated by packing nuts.
Cartridge heater centered in lower stack.

## Slide 27
Thermal runaway
the ‘not so good’
Shipment of Lithium Batteries
Test article: 300 x Lithium –metal CR135 cells pack in one core with a centrally located cartridge heater + insufficient packing media.

## Slide 28
Shipment of Lithium Batteries
And the much better!

## Slide 29
Shipment of Lithium Batteries
Thermal runaway – Post, box dissection
‘spent’ batteries
Loose fill on opening
of box

## Slide 30
Shipment of Lithium Batteries
Layers of cells went into runaway sequentially
All cells consumed over approximately 7 minutes
Thermal runaway – thermal trace

## Slide 31
Shipment of Lithium Batteries
Cells packed in layers, surrounded by Akro protective media
Stage 1:
First ignition (probably by heater) depletes oxygen locally therefore extinguishes the
initial flame (within packaging)
Smoke or mist exits without ignition
Stage 2:
High temperatures, sparks and flame jets retained within the packing material allowing outer surface to remain cool
Surrounding material absorbs heat, preventing it from reaching the outer box
Stage 3:
Propagation to adjacent cells continues , but evolved heat is absorbed by protective media
Thermal runaway – analysis

## Slide 32
9001 Rosehill Road
Lenexa KS USA
+1 913 888 7172
www.akrofire.com
Shipment of Lithium Batteries
Conclusion
The loose fill concept provides a practical and economical method of enhancing the
safety of lithium battery shipments.
R&D is to define parameters which could be used to produce effective shipping scenarios.
ie, quantity of cells to given size of packaging
Loose fill concept is an effective way to ship Lithium battery containing equipment
such as cell phones, computers etc.
Loose fill concept would be an effective and practical method for shipping damaged
and prototype batteries
AkroFire