## Slide 1: The Investigation of a Lithium-Ion Battery Fire Onboard a Boeing 787 - Aspects of the Laboratory Analysis
Joseph Kolly, PhD. Director, Research & Engineering Joseph Panagiotou
Barbara Czech
The Seventh Triennial International Fire & Cabin Safety Research Conference
December 2-5, 2013

## Slide 2: Overview of Presentation
Background of Incident
Battery Design
Investigative Methods
Summary

## Slide 3: Participants
Parties
  FAA
  Japan Airlines
  Boeing Commercial Airplanes
  Thales Avionics Electrical Systems
  GS Yuasa
  JTSB*
  BEA*
Consultants
  NSWC Carderock
  US DOE
  TIAX

## Slide 4: JAL Boeing 787 Logan International Airport –Jan 7, 2013

## Slide 5: Timeline
10:06am - aircraft arrived at gate in Boston from Narita, Japan
  183 passengers and 11 crew deplaned
10:32am - Cleaning and maintenance crew noticed smoke in cabin
10:35am - Mechanic noted flames coming from APU battery in aft electronics bay

## Slide 6: Timeline, cont.
10:37am – Airport Rescue & Fire Fighting notified
10:40am – Fire and rescue personnel arrive on scene
12:19pm – Fire and rescue personnel report event was “controlled”

## Slide 7: Battery Failure as Captured on FDR

## Slide 8: Li-Ion Battery Locations in B-787 (same model battery used in each location)
Main battery
location
Auxiliary Power Unit (APU)
battery location
Lithium Cobalt Oxide
3.7 Volts per cell (nom)
~ 32 Volts total

## Slide 9: Damage to Aft Electronics Bay

## Slide 10: APU and Main Batteries
Exemplar (main) Battery
Incident (APU) Battery

## Slide 11: Component View of Battery

## Slide 12: Battery Specifications
Li-Ion 8 cell battery |  | 
Lithium Cobalt Oxide/Carbon Electrode |  | 
Organic Solvent Electrolyte |  | 
 | Battery | Cell
Nominal capacity (ampere-hour) | 75 | 75
Nominal voltage (volts) | 29.6 | 3.7
Weight (pounds) | 61.8 | 6
Dimensions (inches) |  | 
Width | 10.9 | 5.2
Depth | 14.2 | 2.0
Height | 8.5 | 7.7

## Slide 13: External Observations

## Slide 14: Undamaged Battery with Cover Removed
a
Top Insulator
Removed Lid

## Slide 15: Front View with Top Cover Removed

## Slide 16: Side View with Top Cover Removed

## Slide 17: External “Protrusion”

## Slide 18: External “Protrusion”
Viewed From Outside (Post-clean)
Viewed From Inside (Post-clean)

## Slide 19: SEM/EDS Inspection and Analysis of Protrusion
CRES Elements

## Slide 20: Internal Observations (Battery Level)

## Slide 21: Top View of Battery (cover removed)
APU Battery
Main Battery

## Slide 22: Thermal Damage
Area of most thermal damage
1
2
3
4
8
7
6
5

## Slide 23: Radiography Specifications
Nikon Metrology
450 kV Microfocus scanner
X-ray focal spot size 80 microns
Scan volume 1600 x 1700 x 2000
File size 5.8 - 24 Gb
Post-processing with VGStudio Max

## Slide 24: Mechanical Damage (Digital Radiograph)
1
2
3
4
8
7
6
5

## Slide 25: Inside the Battery
5
6
7
8
4
3
2
1
Moderate thermal damage
Substantial thermal damage
Cells on the left side
Cells on the right side

## Slide 26: Wiring Harness of Battery
Visual examination
Radiographic examination

## Slide 27: Initial Extraction of Cells

## Slide 28: Copper Bus Bars

## Slide 29: Micro-hardness Testing of Bus Bar
Sample Cut for Metallurgical Cross Section

## Slide 30: Battery Monitoring Unit Circuit Boards

## Slide 31: Internal Observations (Cell Level)

## Slide 32: Li-Ion Cell Construction

## Slide 33: Cell #6 External View (CT scan .wmv)

## Slide 34: Side View of Cell 6 (CT scan .wmv)

## Slide 35: Cell #6 CT Scan Showing Current Collector Damage

## Slide 36: Radiographic Image Showing Breach in Cell Case

## Slide 37: Using Dremel Tool to Open Cell Case

## Slide 38: Opened Cell Showing Damaged Electrodes

## Slide 39: Electrode Construction
separator
separator
Al
Cu
Carbon-based material
Li-CoO2-based material
Not to scale
Carbon-based material
Li-CoO2-based material

## Slide 40: Two Sets of Electrodes Unwound in Lab

## Slide 41: Two Sets of Electrodes

## Slide 42: One Electrode “Jellyroll” Unwound
10 feet

## Slide 43: Cell 6 Electrode Damage

## Slide 44: Re-solidified Aluminum on Copper Foil (SEM Image)

## Slide 45: Laboratory Testing
Battery Level
Cell Level
Electrode Level

## Slide 46: Laboratory Testing – Battery Level
Determine uniformity of charging individual cells
Examine thermal distribution during charge/discharge cycles
Determine battery response to charging anomalies

## Slide 47: Laboratory Testing – Cell Level
Examine manufacturing uniformity (Destructive Physical Analysis– DPA)
Test for soft shorts

## Slide 48: Laboratory Testing – Electrode Level
Assembly# of Coin Cell
Cathode Electrode
SS can
SS wave
spring
Gasket
Cu spacer
Cu substrate
Al substrate
Separator
Anode Electrode
Photograph of Coin Cell
Coin-cell testing
  Examine susceptibility to lithium plate out
  Examine uniformity of electrode coatings and anode/cathode ratios

## Slide 49: In Summary,
Investigation of Battery Required Resources Beyond NTSB Internal Capabilities
New Technology - Multiple Sources of Expertise
Fragile and Microscopic Features– Non-Destructive Methods
    Radiography/CT scanning
    Scanning Electron Microscope (SEM)
Material Science and Chemistry Aspects
  SEM/EDS
  FTIR
  Micro-hardness Testing